Crawford 662 SMP Collapsable Curtain Shelter

Product description:

Item curtain shelter 662 SMP

- Frame in extruded aluminium sections

- Front and rear frame spring-loaded and connected with parallel bracing arms

- Self-adjusting roof frame rises automatically independent of the side frames, in case of very high vehicles.

- Continuous wall and roof cover

- Easily replaceable curtains

- Curtain quality

- Top curtain /side curtains:

- Double-layered high quality polyester, coated on both sides

- Total weight approx. 3400 g/m²

- Flammability (DIN 75200)

| Tensile strength: | DIN 53354 longitudinal strength: approx. 7000 N/5cm transverse strength: approx. 5000 N/5cm |
| --- | --- |
| Tear elongation: | DIN 53363 longitudinal strength: approx. 750 N transverse strength: approx. 900 N |

- Continuous roof cover

- One layer high quality polyester, coated on both sides

- Total weight approx. 600 g/m²

- Flammability(DIN 75200)

| Tensile strength: | DIN 53354 longitudinal strength: approx. 2500 N/5cm transverse strength: approx. 2600 N/5cm |
| --- | --- |
| Tear elongation: | DIN 53363 longitudinal strength: approx. 250 N transverse strength: approx. 250 N |

- Top curtain with a slit in the main wear area to minimize contact pressure from the truck

- Installation height 4500 mm above outside yard level

- Standard variants

- Top curtain:

- Top curtain 1000 mm

- Splitted top curtain 1000 mm  (4 slits in the wear area)

- Top curtain 1200 mm

- Splitted top curtain 1200 mm 	(4 slits in the wear area)

- Nominal depth:

- Nominal depth 600 mm

- Nominal depth 900 mm

- Side curtain:

- Side curtain 600 mm (Nominal width 3250 mm)

- Side curtain 700 mm (Nominal width 3450 mm)

- Colour:

- black

- blue (RAL 5010, side and front curtains)

- Colour of parking guides

- white

- yellow (sim. to RAL 1023)

- Wall fixings:

- Concrete

- Sandwich

- ISO panel wall

- Light concrete

- Loadhouse

Dimensions:

|  | mm | Nominal height |
| --- | --- | --- |
|  | mm | Nominal width |

Options:

- Digit on top curtain (Height 300 mm)

- Roof part with integrated rain channel

- Reinforced rubber flaps in the side curtain

- Notching on both sides

- Corner seals to prevent draft in lower area ESR, ES 600, ES 900